Pultrac moulded gratings are manufactured using a heated mould process. Continuous fibres are placed in the mould in alternating layers and are completely wetted out with resin. This continuous process produces an integral, one piece construction which has bi-directional strength. The addition of grit to the surface adds increase slip-resistance.

Pultrac gratings have been developed to meet the stringent quality standards of the American and European markets

Pultrac moulded grating is resistant against corrosion and chemical attack, provide a long lasting safe alternative to metal grating. Available in various dimensions and colours.

| Moulded Grating - Mesh size 38 x 38 mm |  |  |  |  |
| --- | --- | --- | --- | --- |
| Panel Size (mm) | Thickness (mm) | Bar Thickness Top/Bottom | Weight (kg/m2) | Open Area (%) |
| 1220x3660,1220x4000,1220x2440, 915x3050,1268x4010 | 14 | 6.0/5.0 | 6.5 | 78 |
| 1220x3660,1220x4000,1524x4010, 997x3012 | 20 | 6.0/5.0 | 9.8 | 65 |
| 1220x3660,1220x4010,1524x4010, 915x3050,1524x4000,997x3012 | 25 | 6.5/5.0 | 12.3 | 68 |
| 1220x3660,1220x4010,1524x4026, 915x3050,1524x4000 | 30 | 6.5/5.0 | 14.6 | 68 |
| 1220x3660,1220x4000,1200x2440, 915x3050,1524x4000,1524x3050,1000x4000 | 38 | 7.5/5.0 | 19.5 | 68 |
| 1220x4010,1220x3660,1220x2440, 915x3050 | 50 | 11.0/9.0 | 42 | 56 |
| 1220x4010,1220x3660,1220x2440, 1232x4010,915x3050 | 60 | 10.5/9.0 | 50.4 | 54 |
| 1230x4101 | 70 | 11.5/9.0 | 58.8 | 49 |

Uniform Load Deflection

| 8x38x20 | Uniform load deflection Kg/m |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 350 | 500 | 750 | 1000 | 1500 | 2500 | Break point |
| 300 | <0.254 | 0.254 | 0.508 | 0.508 | 1.016 | 1.524 | 29280 |
| 450 | 1.016 | 1.524 | 2.286 | 3.048 | 4.572 | 7.620 | 12980 |
| 600 | 3.084 | 4.572 | 7.112 | 9.398 | --- | --- | 7320 |
| 750 | 5.842 | 8.890 | --- | --- | --- | --- | 7084 |
| 900 | --- | --- | --- | --- | --- | --- | 3226 |

| 38x38x25 | Uniform load deflection Kg/m |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 240 | 480 | 980 | 1450 | 2450 | 3650 |
| 450 | 0.660 | 1.092 | 1.930 | 2.769 | 4.470 | 7.620 |
| 600 | 1.118 | 2.108 | 4.140 | 6.172 | 10.211 | --- |
| 750 | 2.667 | 5.387 | 10.820 | 16.280 | --- | --- |
| 900 | 5.537 | 11.176 | 21.717 | --- | --- | --- |

| 38x38x30 | Uniform load deflection Kg/m |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 350 | 500 | 750 | 1000 | 1500 | 2500 | Break point |
| 300 | <0.254 | <0.254 | <0.254 | <0.254 | 0.254 | 0.508 | 32500 |
| 450 | 0.254 | 0.508 | 0.762 | 1.016 | 1.524 | 2.286 | 21661 |
| 600 | 1.060 | 1.524 | 2.286 | 2.794 | 4.318 | 7.366 | 12980 |
| 750 | 2.540 | 3.810 | 5.842 | 7.620 | 11.684 | --- | 8296 |
| 900 | 4.572 | 7.112 | 10.668 | --- | --- | --- | 5758 |

| 38x38x38 | Uniform load deflection Kg/m |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 240 | 480 | 1450 | 2450 | 3650 | 4880 |
| 300 | 0.254 | 0.305 | 0.381 | 0.457 | 0.635 | 0.838 |
| 600 | 0.432 | 0.813 | 1.549 | 2.311 | 3.835 | 5.740 |
| 900 | 1.702 | 3.454 | 6.659 | 10.465 | 17.475 | --- |
| 1200 | 5.969 | 12.167 | 24.511 | --- | --- | --- |

Line Load Deflection

| 38x38x20 | Line load deflection Kg/m |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 75 | 150 | 300 | 450 | 750 | Break point |
| 300 | 0.254 | 0.508 | 1.016 | 1.524 | 2.540 | 4470 |
| 450 | 0.762 | 1.524 | 3.302 | 4.826 | 8.128 | 2980 |
| 600 | 1.778 | 3.810 | 7.620 | 11.176 | --- | 2235 |
| 750 | 2.794 | 5.588 | 11.430 | --- | --- | 1788 |
| 900 | 5.334 | 10.668 | --- | --- | --- | 1490 |

| 38x38x25 | Line load deflection Kg/m |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 75 | 150 | 300 | 450 | 600 | 750 | Break point |
| 450 | 0.559 | 1.146 | 2.159 | 3.073 | 4.115 | 4.75 | 3910 |
| 600 | 0.864 | 1.702 | 3.505 | 5.156 | 6.706 | 8.179 | 2924 |
| 900 | 2.896 | 5.918 | 12.116 | 18.440 | --- | --- | 1948 |
| 1200 | 5.715 | 111.633 | --- | --- | --- | --- | 1461 |

| 38x38x30 | Line load deflection Kg/m |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 75 | 150 | 300 | 450 | 600 | 750 | Break point |
| 300 | <0.254 | <0.254 | 0.254 | 0.805 | 0.762 | 1.524 | 9923 |
| 450 | 0.254 | 0.508 | 1.016 | 1.524 | 2.540 | --- | 4827 |
| 600 | 0.508 | 1.270 | 2.286 | 3.556 | 5.842 | --- | 4112 |
| 750 | 1.270 | 2.540 | 4.826 | 7.366 | 12.446 | --- | 3173 |
| 900 | 1.778 | 3.810 | 7.620 | 11.430 | --- | --- | 2637 |

| 38x38x38 | Line load deflection Kg/m |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Span (mm) | 75 | 150 | 300 | 450 | 600 | 750 | Break point |
| 300 | 0.279 | 0.365 | 0.483 | 0.610 | 0.762 | 0.889 | 17116 |
| 600 | 0.356 | 0.660 | 1.245 | 1.850 | 2.464 | 3.073 | 8718 |
| 900 | 0.864 | 1.803 | 3.683 | 5.563 | 7.417 | 9.296 | 5817 |
| 1200 | 2.261 | 4.749 | 9.677 | 14.630 | 19.583 | --- | 3755 |